Controlled Drug Release from Large Area Nanoplatforms

Evin Gultepe* 1,2, Dattatri Nagesha1,2,  Srinivas Sridhar1,2

1 Electronics Materials Research Institute Northeastern University, Boston, MA 02115

2 Department of Physics, Northeastern University, Boston, MA 02115

*contact author: gultepe.e@neu.edu

Presentation

Short Description: We show that drugs can be nano-assembled on to biocompatible, non-erodible nanoporous coatings and whose elution kinetics is suitable for drug releasing implants for therapeutic situations.

Keywords: controlled drug release, nanoporous templates, fluorometry, diffusion, desorption

Abstract:

A model drug, doxorubicin, was assembled into large area nanoporous platforms and PCL plugs, and the subsequent release profile was observed by in-situ fluorometry. After an initial burst release phase during the first 100 minutes, a long time sustained release followed for several weeks. The long-time sustained release behavior can be tuned by varying nanotube pore length and diameter. While the sustained release was dominated by non-Fickian diffusion for polymeric platforms, an activated surface density dependent desorption was in effect for nanoporous templates. It has been showed that non-eroding nanoporous coatings of titania or alumina can be used as an alternative to polymeric drug release systems for sustained release over several weeks, see Figure 1.

Figure 1Drug release from nanoporous coatings.

# Footnotes

This work is supported by IGERT Nanomedicine Science and Technology Program (NSF-0504331)