New quantum dot based materials

Y. K. Gun’ko *, M. M. Moloney, S. Gallagher, S. Byrne

The School  of Chemistry and CRANN Institute, Trinity College, University of Dublin, Dublin 2,  Ireland

Quantum dots (QDs) are fluorescent semiconductor (e.g. II-VI) nanocrystals, which have a strong characteristic spectral emission. This emission is tunable to a desired energy by selecting variable particle size, size distribution and composition of the nanocrystals. QDs have recently attracted enormous interest due to their unique photophysical properties and range of potential applications in photonics and biochemistry.The main aim of our work is develop new materials based chiral quantum dots (QDs) and establish fundamental principles influencing the structure and properties of chiral QDs.

Here we present the synthesis and characterisation of various chiral II-VI (CdS, CdSe and CdTe) semiconductor nanoparticles.  The most interesting are   penicillamine stabilised CdS and CdSe nanoparticles, which have shown both very strong and very broad luminescence spectra. Circular dichroism (CD) spectroscopy studies have revealed that the D- and L- penicillamine stabilised CdS and CdSe QDs demonstrate circular dichroism and possess almost identical mirror images of CD signals.1, 2  Studies of photoluminescence and CD spectra have shown that there is a clear relationship between defect emission and CD activity. We believe that these new QDs could find important applications as fluorescent assays and sensors (or probes) in asymmetric synthesis, catalysis, enantioseparation, biochemical analysis and medical diagnostics. Also chiral QDs with an appropriate functionality could potentially serve as materials for the fabrication of circularly polarised light emitting devices. These devices are necessary components of chiroptical detectors used in polarimetry and CD spectrometers. Finally, circular polarized light emitters might have a potential application in colour displays.

References

1. M. M. Moloney, Y. K. Gun’ko, J. M. Kelly, Chem.Comm. 2007, 3900 – 3902.

2. S. D. Elliott, M. P. Moloney and Y. K. Gun’ko, Nano lett , 2008, 8(8), 2452-2457.